Table 3 . Input Parameters of Interface Defect and Absorber Defect.

| Parameters and units | Cs2TiBr6 | ETL/Cs2TiBr6 interface | Cs2TiBr6 / HTL interface |
| --- | --- | --- | --- |
| DEFECT TYPE | NEUTRAL | Acceptor | Acceptor |
| Capture cross section for electron and holes ( cm2 ) | 2.0X10-14 , 2X10-14 | 1.0X10-17 , 1X10-18 | 1.0X10-18 , 1X10-19 |
| Energetic distribution | GAUSSIAN | SINGLE | SINGLE |
| Energy level with respect to EV ( above EV , eV ) | 0.6 | 0.6 | 0.6 |
| Characteristics energy ( eV ) | 0.1 | - | - |
| Total Density ( cm-3 ) | 1.0 X 1013 | 1.0 X 1010 - 1.0 X 1012 | 1.0 X 1010 - 1.0 X 1012 |

| PARAMETERS | Cu20 | CuAlO2 | CuSbS2 | CuSCN | MoO3 | Spiro-OMeTAD | P3HT | PEDOT:PSS | Cs2TiBr6 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness ( nm ) | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 900 |
| BandGap , Eg(eV) | 2.17 | 3.46 | 1.58 | 3.2 | 3 | 3 | 1.85 | 2.2 | 1.6 |
| Electrno affinity X (eV) | 3.2 | 2.5 | 4.2 | 1.9 | 2.5 | 2.45 | 3.1 | 2.9 | 4.47 |
| Realtive Dielectric Permittivity | 7.1 | 60 | 14.6 | 10 | 12.5 | 3 | 3.4 | 3 | 10 |
| CB , Effective density of states Nc ( cm-3 ) | 2.02x1017 | 2.2X1018 | 2X1018 | 2.2X1019 | 2.2X1018 | 1X1019 | 1E+22 | 2.2E+15 | 1E19 |
| VB , effective density of states Nv ( cm-3 ) | 1.1x1019 | 1.8X1019 | 1X10-4 | 1.8X1019 | 1.8X1019 | 1X1019 | 1E+22 | 2.2E+17 | 1E19 |
| Electron mobility ( cm2v-1s-1 ) | 200 | 2 | 49 | 1X10-4 | 100 | 2X10-4 | 1E-4 | 2X10-3 | 4.4 |
| Hole mobility ( cm2v-1s-1) | 80 | 8.6 | 49 | 1X10-1 | 25 | 2X10-4 | 1E-4 | 2X10-3 | 2.5 |
| Shallow uniform donor density ND ( cm-3) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1E+19 |
| Shallow acceptor density NA ( cm-3 ) | 9 X 1021 | 3 X 1018 | 1.38X18 | 1X1015 | 1X1018 | 2X1018 | 3.17E13 | 1E+17 | 1E+19 |
| Total defect density Nt ( cm-3 ) | 1 X 1014 | 1X 1014 | 1 X 1014 | 1 X 1014 | 1 X 1014 | 1 X 1014 | 1 X 1014 | 1 X 1014 | 1 X 1014 |

TABLE 2 INPUT PARAMETERS OF HTLs.

TABLE 1 INPUT PARAMETERS OF ETLs

| PARAMETERS | FTO | TiO2 | Zno | STO | IGZO | PCBM | Znse | CdS | WO3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness ( nm ) | 500 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | 30 |
| BandGap , Eg(eV) | 3.2 | 3.2 | 3.3 | 3.2 | 3.05 | 2 | 2.81 | 2.4 | 2.92 |
| Electrno affinity X (eV) | 4.4 | 3.9 | 4.1 | 4.0 | 4.16 | 3.9 | 4.09 | 4.18 | 4.590 |
| Realtive Dielectric Permittivity | 9 | 9 | 9 | 8.7 | 10 | 4 | 8.6 | 10 | 5.76 |
| CB , Effective density of states Nc ( cm-3 ) | 2.2X1018 | 1X1021 | 4X1018 | 1.7X1019 | 5X1018 | 1X1021 | 2.2X1018 | 2.2X1018 | 1.96X1019 |
| VB , effective density of states Nv ( cm-3 ) | 1.8X1019 | 2X1020 | 1X1019 | 2X1020 | 5X1018 | 1.8X1019 | 1.8X1018 | 1.9X1019 | 1.96E19 |
| Electron mobility ( cm2v-1s-1 ) | 90 | 20 | 100 | 5.3X103 | 15 | 1E-2 | 4x102 | 100 | 1E+1 |
| Hole mobility ( cm2v-1s-1) | 90 | 10 | 25 | 6.6X102 | 0.1 | 1E-2 | 1.1x102 | 25 | 1E+1 |
| Shallow uniform donor density ND ( cm-3) | 7X102 | 1X1019 | 1X1018 | 2X1016 | 1X1018 | 1E+20 | 1x1018 | 1X1018 | 3.68E+19 |
| Shallow acceptor density NA ( cm-3 ) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| Total defect density Nt ( cm-3 ) | 1X1014 | 1X1014 | 1X1014 | 1X1014 | 1X1014 | 1X1014 | 1X1014 | 1X1014 | 1X1014 |

| Structure of PSCs | Voc ( V ) | Jsc (mA/cm2) | FF ( % ) | PCE( % ) |
| --- | --- | --- | --- | --- |
| Au/ CUALO2 / Cs2TiBr6 / IGZO/FTO | 1.1231 | 23.543828 | 73.88 | 19.53 |
| Au/ CUALO2 / Cs2TiBr6 / ZNO/FTO | 1.1231 | 23.543129 | 73.86 | 19.53 |
| Au/ CUALO2 / Cs2TiBr6 / TIO2/FTO | 1.1267 | 23.546622 | 72.46 | 19.22 |
| Au/ CU2O / Cs2TiBr6 / ZNSE/FTO | 0.6726 | 23.54986 | 69.26 | 10.97 |
| Au/CU2O/ Cs2TiBr6 / PCBM/FTO | 0.6732 | 23.551993 | 68.38 | 10.84 |
| Au/ CU2O / Cs2TiBr6 / TIO2/FTO | 0.6727 | 23.549836 | 67.41 | 10.68 |
| Au/ CU2O / Cs2TiBr6 / ZNO/FTO | 0.6614 | 24.16615 | 64.38 | 10.29 |
| Au/ MOO3 / Cs2TiBr6 / CDS/FTO | 0.6582 | 23.551529 | 60.16 | 9.33 |
| Au/ MOO3 / Cs2TiBr6 / ZNO/FTO | 0.6579 | 23.546039 | 60.16 | 9.32 |
| Au/ MOO3 / Cs2TiBr6 / TIO2/FTO | 0.6582 | 23.549529 | 58.43 | 9.06 |